## Slide 1: Understanding OLED Dynamics on Multiple Time Scales
Kyle W. Hershey
Department of Chemical Engineering & Materials Science
University of Minnesota, Minneapolis, MN
Funding provided by The Dow Chemical Company

## Slide 2: Personal Background
From:
  Stoughton, WI
Undergraduate Education (2009-2013):
  Coe College (Cedar Rapids, IA)
  Majors:
    Physics
    Mathematics
    Computer Science
Graduate Education (2013-Present):
  University of Minnesota
  Materials Science and Engineering
  Advisor:
    Prof. Russell Holmes
  Research:
    Organic Light Emitting Devices (OLEDs)
1
2
3
4
5

## Slide 3: Outline
OLED background
  Overview and applications
  Operation
  Challenges
Device Physics
  Efficiency roll-off at high current
  Transient electroluminescence
  Analytical formalism for “charge balance”
Lifetime and Test Engineering
  Degradation as efficiency loss
  Extracting dynamics
  Design rules for long lifetime
Data Engineering
  Measurement system integration
  Analysis Capabilities
  Machine Learning

## Slide 4: Outline
OLED background
  Overview and applications
  Operation
  Goals
Device Physics
  Efficiency roll-off at high current
  Transient electroluminescence
  Analytical formalism for “charge balance”
Lifetime and Test Engineering
  Degradation as efficiency loss
  Extracting dynamics
  Design rules for long lifetime
Data Engineering
  Measurement system integration
  Analysis Capabilities
  Machine Learning

## Slide 5: OLEDs
Highly Commercialized
  Mobile displays
  Large format displays
  Architectural Solid-State Lighting
Unique Features
  High efficiency
  Unmatched contrast
  Wide color gamut
    Tunable emission
  Thin form factor
  Flexible substrate compatible
Apple 2017
Google 2017
Samsung 2017
LG 2016
Acuity

## Slide 6: What are OLEDs?
Transparent conducting oxide (ITO) for light emission
Thin films produced with vacuum or solution processing
Organic conjugated small molecules
Ir(ppy)3
CBP
TPBi
NPD
Alq3

## Slide 7: Films and processing
Spin coated hole injection layer
  PEDOT-PSS
Thermal vapor deposition
  Sublimation
  P< Torr
  Mixures are Codeposited
50-150
Molecular Weight: 300-800
Amorphous
  Van der Waals bonding
  Recent efforts in enhancing density and morphology
http://advancedcoatings.nagasechemtex.co.jp/en/images/about/pedot_img.png

## Slide 8: Organic Semiconductors
Conduction by hops between discrete molecules
Highest Occupied Molecular Orbital (HOMO)
  Think valence band
Lowest Unoccupied Molecular Orbital (LUMO)
  Think Conduction Band
Excitons
Coulombically bound electron-hole pair
Charges bound on single molecule
Lifetimes 10 ns – 100 ms
Main conceptual deviation from traditional LEDs
CBP

## Slide 9: OLED Operation
Charges (polarons) move through transport layers (HTL/ETL)
Charges combine to form excitons
  Emissive layer (EML)
  Profile of exciton formation called recombination zone
Excitons emit light
Notes: Molecultes primarily composed for carbon, nitrogen, hydrogen
Ir used for increased photoconversion efficiency

## Slide 10: Efficiency Components
Photons out per electron in
= Charge Balance
= Radiative Spin Fraction
= Photoluminescence Efficiency
= Out-Coupling Efficiency
η=

## Slide 11: Active Research Fields
Focused on two problems:
Efficiency reduces at high brightness
Degradation over time
Steady-State
Lifetime
Roll-off
Both limited by understanding of kinetics

## Slide 12: Outline
OLED background
  Overview and applications
  Operation
  Goals
Device Physics
  Efficiency roll-off at high current
  Transient electroluminescence
  Analytical formalism for “charge balance”
Lifetime and Test Engineering
  Degradation as efficiency loss
  Extracting dynamics
  Design rules for long lifetime
Data Engineering
  Measurement system integration
  Analysis Capabilities
  Machine Learning

## Slide 13: Motivation
Existing models predict efficiency roll-off using quenching
  Magnitude unknown
  Low current behavior not predicted
Existing Model is Incomplete
Exciton-Exciton Annihilation
Exciton-Polaron Quenching

## Slide 14: Further Limitations
Typically only analyzed in steady-state
Dynamics are also expressed in transient voltage response
  Existing model fails in this regime
Roll-off
Transient
Steady-State

## Slide 15: Exciton Kinetics
Key Processes:
  Exciton Formation
    From injected polarons
    NOT instantaneous
    Competitive with leakage
  Exciton Recombination
    Radiative emission
    Competitive with quenching
Exciton Lifetime
Exciton-Exciton Annihilation
Exciton-Polaron Quenching
Exciton Formation
Need to include polaron dynamics

## Slide 16: Model Summary
Polaron leakage
Analysis Strategy:
  Fit transient electroluminescence without polaron leakage
    Valid while shorter than voltage pulse
  Introduce polaron leakage to replicate entire efficiency profile
Exciton Lifetime
Triplet-Triplet Annihilation
Triplet-Polaron Quenching
Exciton Formation
Exciton Formation
Polaron Injection

## Slide 17: Transient Electroluminescence
Model fits both the rise and fall of the decay
is the only new parameter
Delay after beginning of pulse is accounted for with polaron injection and transport time

## Slide 18: Transient Electroluminescence

## Slide 19: Deconstructing Efficiency
Charge balance can be defined as exciton formation efficiency ()
accounts for the rise in at low current density
Onset of roll-off accounted for with quenching
contributes to roll-off at high current density

## Slide 20: Summary
Developed model to universally fit transient and steady-state electroluminescence
  Exciton formation rate () and polaron transit time ()
Exciton formation efficiency defined naturally from polaron dynamics
Full dynamics allow understanding of exciton formation and efficiency

## Slide 21: Outline
OLED background
  Overview and applications
  Operation
  Goals
Device Physics
  Efficiency roll-off at high current
  Transient electroluminescence
  Analytical formalism for “charge balance”
Lifetime and Test Engineering
  Degradation as efficiency loss
  Extracting dynamics
  Design rules for long lifetime
Data Engineering
  Measurement system integration
  Analysis Capabilities
  Machine Learning

## Slide 22: OLED Degradation
OLED degradation remains a key area for improvement, especially in blue- and white-emitting devices
Difficult to optimize due to long testing time, even when accelerated
Minimal extracted data
Degradation mechanisms poorly understood - Convolution of dynamics
Hershey et. al. Appl. Phys. Lett. 2017, 111, 113301.

## Slide 23: Decoupling Efficiency Losses
Luminance loss is loss in efficiency
η=ηOCχ
Exciton formation () includes leakage (charge balance) as well as losses to non-radiative recombination centers
Can decouple if we can measure independently
  Previously not possible

## Slide 24: Deconstructing OLED Degradation
Intermittent optical excitation to probe only guest photoluminescence
Optical excitation does not degrade device
Separate measurements confirm that PL is the same as
EL
PL
EL Lifetime (Hours)
Continuous EL
(10 minutes)
PL (~20 seconds)

## Slide 25: Deconstructing OLED Degradation
Intermittent optical excitation to probe only guest photoluminescence
Optical excitation does not degrade device
Separate measurements confirm that PL is the same as
EL
PL
EL Lifetime (Hours)
Continuous EL
(10 minutes)
PL (~20 seconds)

## Slide 26: Deconstructing OLED Degradation
Laser signal is split among six devices
Software synchronizes EL and PL measurements and controls current
Lifetime is within error with and without PL breaks
Laser
Laser Optics
Laser Power Meter
Device Holders
Detection Switcher
Current Sources
Laser Controller
Measurement Unit

## Slide 27: Software Interface
Expansive software allows for multiple testing conditions
Constant current, optical degradation, intermittent laser probes, etc
Configurable to multiple hardware setups
Written in Python
Stores results in searchable database

## Slide 28: Deconstructing OLED Degradation
Additional data acquired from same test on same device
Exciton formation and emission losses can be separated using a single run
Device limitations are immediately identified!
Hershey et al., Appl. Phys. Lett. 2017, 111, 113301.

## Slide 29: Application to Device Optimization
Investigating EML thickness dependence of lifetime
  Significant lifetime improvement for 30 nm
PL loss is mostly independent of EML thickness
  Suggests minimal change in exciton density
  Similar recombination zone width
Degradation in exciton formation determines time scale of EL decay

## Slide 30: Probing the Recombination Zone
Previous studies have recombination zone pinning to accelerate degradation
This acceleration is also observed in our data
  Only changes the decay
Measurements have shown that the recombination zone is pinned at the TPBi interface in the 10 and 20 nm EML devices

## Slide 31: Technique Applications
PL degradation scales with thickness
Exciton density scales with EML thickness
Recombination zone causing lifetime enhancement
J. S. Bangsund, K. W. Hershey, R. J. Holmes, ACS Appl. Mater. Interfaces 2018
LiF + Al
TCTA:TPBi:Ir(ppy)3 (5%)
X nm
TPBi 20 nm
TCTA 20 nm
AQ1200/ITO/Glass
TCTA
TPBi

## Slide 32: Technique Applications
Collaboration with Dow
Improved performance from cohost system
  Often due to more balanced charge transport
  In this system, Host A is less conductive for both carriers
Lifetime is a balance of recombination zone and interfacial effects
Previous two studies demonstrate end points of this scale
K. W. Hershey, J. S. Bangsund. 2018. (In Preparation)

## Slide 33: Summary
Developed decoupling technique for lifetime
Separate parameters help design process
Recombination zone important for degradation
  RZ position
  RZ width and exciton density

## Slide 34: Outline
OLED background
  Overview and applications
  Operation
  Goals
Device Physics
  Efficiency roll-off at high current
  Transient electroluminescence
  Analytical formalism for “charge balance”
Lifetime and Test Engineering
  Degradation as efficiency loss
  Extracting dynamics
  Design rules for long lifetime
Data Engineering
  Measurement system integration
  Analysis Capabilities
  Machine Learning

## Slide 35: Data Collection Techniques
Our lab collects large datasets
  Fewer experiments
  Lots of data along with it
Difficult to compare and keep track
I have used my background to improve data collection and usage
  Integrated collection and organization into measurement tools
  Data storage in database
  Reworked analysis protocol
  Enabled machine learning applications

## Slide 36: Data in Our Lab
Growth Information
    Layer stack of materials
    Lab conditions
Characterize devices/films
    Spectral
    Current-Voltage
Lifetime Testing
    Testing conditions
    X vs Time

## Slide 37: Data in Our Lab
Characterize devices
  Experiment details and data collected within measurement software
  Analyzed results immediately available through web interface
Lifetime Testing
  Integrates with device data to set driving current
Instrument Uploaders
  Allows easy integration of data at time of testing

## Slide 38: Comparing Data
Architecture and growth browser allow easy comparison of datasets
Plots common measurements

## Slide 39: Programmatic Data Access
All data searchable by key parameters
Trend recognition / Model development
  Lifetime has functional dependence on exciton density
    Matches luminance and
Visualization
  Less useful, but still cool
J. S. Bangsund, K. W. Hershey, R. J. Holmes, ACS Appl. Mater. Interfaces 2018

## Slide 40: Machine Learning
Bad pixel recognition
  Used pre-labeled “bad” devices to recognize unrepresentative scans
Spectral recognition
  Trained on emitters known to our group
  What is this unknown molecule:
    A 80% match
    B 20% match
  Want to expand to recognizing impurity molecules and impure spectra
A
B

## Slide 41: Conclusions
Device Physics
  Developed understanding of charge dynamics
  Quantified definition of exciton formation efficiency
Lifetime and Test Development
  Developed method for decoupling degradation
  Manufactured hardware and software to enable test
  Used method to understand lifetime improvements
Data Engineering
  Collected lab data into database using testing software suite
  Revolutionized data analysis
  Incorporating machine learning

## Slide 42: Questions?
Kyle Hershey
kwhershey@gmail.com

## Slide 45: Archive Search Tools
All spectral measurements previously done by group imported
Searchable from web interface
Easy access to reference data
Wavelength (nm)
Intensity

## Slide 46: Conclusions
Unification of transient / steady-state dynamics
  Developed understanding of charge dynamics
  Quantified definition of exciton formation efficiency
Decoupling operational lifetime
  Developed method for decoupling degradation
  Used method to understand lifetime improvements

## Slide 47: Correctly Probing
For a measurement of PL intensity to reflect , exciton generation (guest absorption) must be constant during degradation:
Can confirm with exciton decay
kinetics:

## Slide 48: Accounting for Polaron Dynamics
Exciton Formation
  Electrons and holes may combine to form an exciton
  Spatially averaged exciton formation rate
  is exciton formation rate constant
Polaron Loss
  Polarons have a finite residence time due to transit through the emissive layer
More complete picture requires polaron dynamics
K. W. Hershey, R. J. Holmes, J. Appl. Phys. 2016, 120, 195501.

## Slide 49: Deconstructing Efficiency
Previous model fit normalized roll-off
I used polaron leakage () to create exact fit
Polaron leakage is not arbitrary
  Agrees with carrier drift through emissive layer under applied field

## Slide 50: Initial Attempts
Need to measure
Excite device before and after using 405 nm laser
  Only probes emitter
  Luminance ratio is loss in
Each curve requires one device for every point
Error
  Sample to sample
  Measurement reproducibility
Want all information from one device without moving
EL
EL
EL
PL
PL
PL

## Slide 51: Application to Device Optimization
How can we use this method to understand device performance and optimization?
Increase in lifetime with EML thickness - What is causing this improvement?
TPBi
Ir(ppy)3
CBP
AlQ3
NPD

## Slide 52: Application to Device Optimization
How can we use this method to understand device performance and optimization?
Increase in lifetime with EML thickness - What is causing this improvement?

## Slide 53: Application to Device Optimization
Recombination loss is mostly independent of EML thickness
  Invariance suggests minimal change in exciton density
  Similar recombination zone width
Degradation in exciton formation determines time scale of EL decay
5000 cd/m2
1000 cd/m2