## Slide 1: Dow Host A and B Lifetime Update and Identifying Trends with Host Energetics and Device Stability
John Bangsund
Kyle Hershey
2017-11-20

## Slide 2: Efficiency with Standard Transport Layers
Efficiencies are lower across the board
  May be due to too high doping of Ir(ppy)3, reducing
Host A performs significantly better
  Suggests transport layers are better aligned for injecting into Host A
LiF + Al
Host:Ir(ppy)3 (15%) 40 nm
TPBi 30 nm
TCTA 20 nm
AQ1250/ITO/Glass

## Slide 3: Energy Levels
LUMO of Host A and B taken as HOMO + Eg
Reduced hole-injection barrier for TCTA/Dow A
  May explain difference in EQE roll-up
Could use TAPC or NPD, which have shallower HOMOs of 5.4 – 5.5 eV

## Slide 4: Lifetimes
Lifetimes are shorter than previously, limited by transport layers
Host B shows the worst PL degradation
Host A shows the worst degradation
Co-Host selects the best of both hosts
Driving voltage rise appears correlated with
  Could suggest that trapped charge increases polaron quenching (which is lumped in with )
  Or could suggest that shifting injection barriers leads to both voltage rise and exciton formation loss

## Slide 5: Triplet Energies
We are now able to measure triplet emission
Delayed phosphorescence spectra
  10 K Cryo Station
  5 ms after excitation
  Similar turn on
    ~2.6 eV
  Host B has less pronounced features

## Slide 6: Hypotheses on Role of Host A
Host A slows down hole transport/injection into the EML
  Improves charge balance and broadens recombination zone
Next steps:
  Measure lifetime of devices with low concentration of Ir(ppy)3
  Measure mobility of Host A and Host B
  Measure recombination zone
Host A+B
Host B

## Slide 7: Host Comparisons
We want to look at the importance of host on lifetime
  What properties of the host affect device lifetime?
  Will we see changes in or exciton formation efficiency ()?
  Can we predict these changes based on properties of molecules?
Will look at the carbazole family of hosts as a preliminary study
  Multiple close analogues readily available - Start with CBP and mCP
ITO/Glass
TCTA – 40 nm
Host:Irppy 6%– 20 nm
TPBi– 40 nm
LiF/Al
CBP
mCP
CDBP
BCBP

## Slide 8: Device Statistics
CBP EQE is only significant outlier in EQE
Two hump current-voltage and luminance-voltage for all

## Slide 9: Lifetime Data

## Slide 10: Trends
No conclusive trends

## Slide 11: Future Work - Hosts
No clear trends with EL behavior between hosts
Want to look at optical only degradation
  Simpler degradation
  Simpler architectures
    Just host and emitter
  Hypothesis:
    Excess energy increases degradation rate
      Would trend with Triplet Energy
      Unknown if pump wavelength matters

## Slide 12: Exciplex Forming Co-Hosts
[1] B. S. Kim, J. Y. Lee, Adv. Funct. Mater. 2014, 24, 3970. [2] Y.-S. Park et al. Adv. Funct. Mater. 2013, 23, 4914.
Exciplexes are an emissive state that form between the LUMO of an acceptor and the HOMO of a donor
Exciplex energy can be readily tuned by changing either the donor or the acceptor
How does energy of co-host exciplex affect degradation?
D
A

## Slide 13: Exciplex Co-Hosts: Electrical Degradation
mCP-TPBi shows slightly better stability in PL than TCTA-TPBi
TCTA-B3PYMPM has dramatically lower lifetime
  Could be due to morphological instability
  B3PYMPM appears to crystallize easily
Need to compare across a wider range of co-hosts to see if trend emerges
TCTA 35 nm
Co-Host:Ir(ppy)3 (5%) 30 nm
TPBi 35 nm
AQ1250/ITO/Glass
Li-acac + Al
L0=1,000 cd/m2

## Slide 14: Exciplex Co-Hosts: Optical Degradation
To simplify comparisons, we compared degradation under optical excitation
  Reduces complexities due to charge carriers and differences in recombination zone
Devices are illuminated with 405 nm laser
Power generates an exciton density equivalent to ~500 cd/m2
Same general trend is seen
405 laser
Detector
Beam expander

## Slide 15: Exciplex Co-Hosts: Future Work
Not clear if lifetime differences are due to co-host properties or limited by morphological stability
Study wider range of co-host pairs
Continue studying optical degradation
  Influence of pump wavelength (pump guest and host)
  Influence of pump power density
Study role of charge carriers with single-carrier devices