## Slide 1: Efficiency, lifetime, and energy levels
(a)
(c)
(d)
(e)
Figure 1. Efficiency and Energy Levels
(a) External quantum efficiency (EQE) as a function of current density for various Host A and Host B blend ratios. (b) Peak EQE and turn-on voltage (at 1 cd/m2) as a function of host compostion. (c) and (d) Current density and luminance as a function of voltage for various host compositions. (e) Energy level schematic illustrating the HOMO, LUMO, and triplet energy levels for the materials used in these devices. The x-axis denotes the layer thicknesses used in these devices, as a function of distance from the HTL/EML interface.
(b)

## Slide 2
Figure 2. 10 nm EML Lifetimes
(a)
(b)
(a)
(b)

## Slide 3
Dow Hosts:Ir(ppy)3 (15%) 100 nm
TCTA (30 nm)
Al 100 nm
ITO
TCTA 30 nm
MoOx 10 nm
Dow Hosts:Ir(ppy)3 (15%) 100 nm
TPBi (30 nm)
LiF 1 nm/Al 100 nm
ITO
TPBi 30 nm
LiF 1 nm/Al 10 nm
Electron Only
(a)
(b)
(c)
(d)

## Slide 4
Figure 4. 10 nm EML Lifetimes
(a)
(b)

## Slide 5
TCTA
TPBi
2.4
5.7
2.8
6.1
Dow B
2.4
5.3
Dow A
2.3
5.7
T1 = 2.8
T1 = 2.8
Ir(ppy)3
2.6
5.1
T1 = 2.4
T1 = 2.6
T1 = 2.85
x (nm)
-20
0
40
70
LiF + Al
Host:Ir(ppy)3 (15%) 40 nm
TPBi 30 nm
TCTA 20 nm
AQ1250/ITO/Glass

## Slide 6: SI: Host properties
(a)
(b)

## Slide 7: SI: RZ measurement spectra

## Slide 8: SI: 10 nm M-EML Efficiencies

## Slide 9: Electric field profiles

## Slide 10: SI: 5% Ir(ppy)3 Devices