## Slide 1: Origin of Lifetime Enhancement in Mixed Emissive Layer Organic Light-Emitting Devices
John Bangsund

## Slide 2: Paper figure outline
Device architecture, EQE
RZ measurement
EL, PL, and gamma vs t for fixed luminance and scaled luminance
t85 PL and gamma vs L0 and 1/dEML (add third subfigure with gamma t85, t75, t60 vs 1/dEML to show change in slope?)
The maximum published width for a one-column figure is 3.37 inches (8.5 cm). The maximum width for a two-column figure is 6.69 inches (17 cm).

## Slide 3: 1. Device Architecture, EQE and Lifetime
Figure 1 - Suddard-Bangsund et al.
Notes: Figure 1. a) Device architecture schematic for M-EML devices employed in this work. The HTL/M-EML/ETL thickness is kept constant at 100 nm by varying the transport layer thicknesses equally, and the M-EML width (dEML) is varied from 10 to 60 nm. b) EQE characteristics as a function of EML thickness. Peak EQE increases slightly at higher EML thickness, and the onset of roll-off is also delayed to higher current densities.
All data from 2-16-17

## Slide 4: 3. EL-PL thickness dependence
Figure 3 - Suddard-Bangsund et al.

## Slide 5: 4. EL+PL: Exciton Density Scaling
Figure 4 - Suddard-Bangsund et al.
Notes: Figure 3. (a) Normalized electroluminescence (EL) intensity for 10, 30, and 60 nm M-EML devices operated at an initial luminance of 3 kcd/m2. The current densities for these tests were 7.2, 6.4, and 6.0 mA/cm2, respectively. (b) The decoupled photoluminescence (PL, symbols) and exciton formation efficiency losses (, solid lines) corresponding to the curves in (a). (c) Decoupled PL and losses for 10, 30, and 60 nm M-EML devices operated at 1, 3, and 6 kcd/m2, respectively. The current densities for these tests were 2.0, 6.0, and 12.0 mA/cm2, respectively.
Figure 3. (a) Normalized electroluminescence (EL) intensity for 10, 30, and 60 nm M-EML devices operated at an initial luminance of 3 kcd/m2. The current densities for these tests were 7.2, 6.4, and 6.0 mA/cm2, respectively. (b) The decoupled photoluminescence (PL, symbols) and exciton formation efficiency losses (𝛾, solid lines) corresponding to the curves in (a). (c) Decoupled PL and 𝛾 losses for 10, 30, and 60 nm M-EML devices operated at 1, 3, and 6 kcd/m2, respectively. The current densities for these tests were 2.0, 6.0, and 12.0 mA/cm2, respectively.

## Slide 6: 5. t50 vs. L0 and 1/dEML
Figure 5 - Suddard-Bangsund et al.
alternative:
Notes: Figure 4.

## Slide 7: 2. Recombination Zone Measurement
Figure 2 - Suddard-Bangsund et al.
Notes: Figure 2. a) Counts-normalized electroluminescence spectra for sensitized 60 nm M-EML devices at J = 1 mA/cm2 with sensitizer doped strips centered at 5, 15, 30, 45, and 55 nm from the HTL. b) Normalized exciton density profiles for 0.1, 1, and 10 mA/cm2. Solid lines are guides to the eye. Error bars in position represent the width of the dopant strips and the Förster radius between Ir(ppy)3 and PtTPBP (3.7 nm). Error bars in relative exciton density represent standard deviations taken from a minimum of four samples. c) Electric field profile of the PL pump (λ = 405 nm) and the spectrally-weighted outcoupling efficiency for Ir(ppy)3 emission.

## Slide 8: SI Figures

## Slide 9
Energy
TPBi
TCTA
5.7
2.4
6.1
2.8
5.1
2.6
4.8
2.9
Ir(ppy)3
PtTPBP
PtTPBP
T1 = 1.6 eV
R0=3.7 nm
(a)
(b)

## Slide 11
a mismatch factor of sorts could be calculated as:
(a)
(c)
(d)
(b)

## Slide 12
(a)
(b)

## Slide 13
Choice of / influences estimates of